- PermaTill Base Applications For Existing Clay Soil

2.1 Product

A.        STALITE  PermaTill Rotary Kiln Expanded Slate

1.  ASTM C29 Unit Dry Weight loose (52 lb./cf to 55 lb./cf)

2. ASTM C127 Specific Gravity to meet 1.45 to 1.60, SSD

STALITE PermaTill Expanded Slate

(5/16”) PermaTill Expanded Aggregate

Sieve Size        % Passing

½”                               100

3/8”                      80 - 100

#4                          5 - 40

#8                            0 - 20

#16                          0 - 10

5.  Absorption  (ASTM C127)  5 to 9 %

6. The expanded slate must contain no clay lumps or any organic impurities.

2.2 Tilling PermaTill Into Existing Soil

- Using a mechanical tiller.

  - Kill any undesirable vegetation with approved herbicide.

  - Remove dead vegetation and other debris.

  - Subsoil, disk or till soil to a depth of 8” to 12”

  - For a  35% to 50% amendment:  place 2 to 4 inches of PermaTill over the entire area to be planted depending on clay content.

  - Using a tiller, completely till the four inch layer of PermaTill into the soil.

  - Rake the surface smooth and install sod as specified.